## Slide 1: Intelligent Selection and Rational Co-Design of AM Polymers for Marine Applications
Carly Travis
Applied Masters Student
Materials Science and Engineering
University of Washington

## Slide 2: Polymer co-design for FDM additive manufacturing
Goal: select + design thermoplastic materials for AM that will have superior resistance to marine degradation
  Polymers have near-infinite chemical spaces and property variables, making “trial-and-error” approaches ineffective in covering all possibilities
Solution: data and simulation-driven approach to selection + design
  Screen polymers/monomers within datasets based on property objectives
  Model chains in simulated marine environments and extract data
  Validate model via experiments with accelerated degradation protocol
Why: Reduce experimental time + resources
  Accelerate materials development + Discover unique material solutions
  Provide framework for future material needs

## Slide 3: Polymer marine degradation mechanisms
Polymer degradation is influenced by chemical sequence
  Changes at molecular level can reduce functionality of bulk structure (printed part)
Utilize data science to reveal molecular structure-property-performance trends influencing degradation through:
  Datasets
  Simulation
  Validation
Influence of monomer structure on plastic degradation in marine environments
Chemical, structural, physical
Polymer Properties
Prediction + Selection
Degradation probability
Method

## Slide 4: Specific aims for approach:
Aim 1
Construct + screen property datasets to find best candidates
Simulate best candidates to reveal molecular-scale degradation mechanisms
Uncover structure-property trends and predict when/why degradation occurs
Aim 2
Validate and guide models via in-person experimentation
Aim 3
Supplemental Aims
Incorporate additives (CF/chemical)
Model UV + biofilm mechanisms
Simulation-guided design for new properties (i.e. conductivity)
Aims +
Screen candidates based on property objectives + reveal structure-property- performance trends
Expose polymers to equivalent degradation environments in simulation and laboratory

## Slide 5: Aim 1 - Data science applied to polymer properties
Dataset constructed from multiple open-source sets of thermophysical property information
  Organized according to monomer unit
Literature + theory-guided property selection of 5 general parameters for screening:
Aims to reveal structure-property trends in degradation and best candidates for AM

## Slide 6: Aim 1 - Data science applied to polymer properties
Distributions of density, molecular weight, melting temperature, and glass transition temperature data in the studied within dataset of interest for marine degradation. Correlation plots between different properties of interest for each category are modeled.
Polymers with similar monomer structures tend to have similar property distributions

## Slide 7: Aim - 2: Simulations of marine degradation - method
LAMMPS used for simulating marine degradation:
  Polymer chain
  Water molecules
  3.5% salt ions
Set to accelerated degradation protocol used in laboratory
  Temperatures range 20-70C
  Duration of 2 and 4 weeks
Post-simulation results are compared to initial data to reveal extent of property change and the mechanisms by which they changed
Chemical Composition
Molecular Weight
Tg Tm
Density
Properties Evaluated in LAMMPS

## Slide 8: Aim 3 – Validate models through experimentation
Perform accelerated aging of AM polymers to guide and validate methods of Aim 1 and Aim 2.
  Current work: Polyphenylene Sulfide (PPS)
    Engineering AM polymer with excellent thermal and chemical stability
Experiment
Chemical composition via Raman
Thermal properties via TGA, DSC
Simulation
Chemical composition changes visualized
Density + volume used to approximate thermal properties
Bulk property change via tensile test
Water absorption via mass gain
Water absorption via surface area change
PPS monomer 2D to 3D representation, modeled in Avogadro for LAMMPS
Future candidates: ULTEM, Nylon (PA)

## Slide 9: Building and modeling PPS simulation

## Slide 10: Validating unaged PPS composition via Raman
Peak [cm-1] | Component
1577, 629 | C-C (phenyl)
1181 | C-H
1077 | C=CH (benzene)
743 | C-S

## Slide 11: Validating PPS composition after aging
  Marine exposure at these temperatures has little influence on chemical composition over 14/28 day periods
Minor change for:
  C-C phenyl group (1577 cm-1)
  C-S bonds (743 cm-1)
No change for C=C benzene ring (1077 cm-1)
We should expect to see minimal change in chemical groups during simulation
PPS aged in seawater at temperatures of 50, 70C for 14 and 28 days

## Slide 13: UTS - Aged 14 Days
Temp (℃) | 30 | 50 | 70
UTS (MPa) | 47.37 | 50.05 | 52.81
STDEV | 1.23 | 1.13 | 1.31

## Slide 14: UTS - 28 Days
Temp (℃) | 50 | 70
UTS (MPa) | 35.47 | 43.79
STDEV | 1.41 | 9.56

## Slide 15: Overall Comparison UTS

## Slide 18: Relaxation Procedure